New Project

User name: Phenom-World-PC\Phenom-World

Contains 4 images with a total of 4 analyses

01. Image 1

1 analysis: 1x linescan

02. Image 2

1 analysis: 1x linescan

03. Image 3

1 analysis: 1x map

04. Image 4

1 analysis: 1x linescan

Image 1

1. linescan

|  | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 82; Pb; Lead; 24.23; 59.26. 26; Fe; Iron; 40.09; 26.43. 24; Cr; Chromium; 9.11; 5.59. 28; Ni; Nickel; 5.93; 4.11. 8; O; Oxygen; 15.19; 2.87. 13; Al; Aluminium; 5.45; 1.74. |
| --- | --- |

FOV: 20.9 µm, Mode: 15kV - Map, Detector: BSD Full, Time: FEB 1 2023 08:01

Disabled elements: B, F, La

Cut out of line scan (resolution: 512 points)

| Iron | Lead | Oxygen |
| --- | --- | --- |
| Chromium | Nickel | Aluminium |

Combined line scan

Image 2

1. linescan

|  | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 26; Fe; Iron; 41.29; 34.99. 82; Pb; Lead; 10.98; 34.52. 28; Ni; Nickel; 13.14; 11.71. 24; Cr; Chromium; 12.43; 9.81. 8; O; Oxygen; 14.68; 3.56. 13; Al; Aluminium; 6.63; 2.71. 83; Bi; Bismuth; 0.85; 2.70. |
| --- | --- |

FOV: 19.9 µm, Mode: 15kV - Map, Detector: BSD Full, Time: FEB 1 2023 08:06

Disabled elements: B, F, La, S

Cut out of line scan (resolution: 512 points)

| Iron | Oxygen | Nickel |
| --- | --- | --- |
| Chromium | Lead | Aluminium |
| Bismuth |  |  |

Combined line scan

Image 3

1. map

| Combined map | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 82; Pb; Lead; 18.67; 52.32. 26; Fe; Iron; 39.87; 30.11. 24; Cr; Chromium; 9.81; 6.90. 28; Ni; Nickel; 5.78; 4.59. 8; O; Oxygen; 12.95; 2.80. 13; Al; Aluminium; 5.88; 2.14. 6; C; Carbon; 7.04; 1.14. |
| --- | --- |

FOV: 16.8 µm, Mode: 15kV - Map, Detector: BSD Full, Time: FEB 1 2023 08:14

Disabled elements: B, F, La

Cut out of map (resolution: 102x128 pixels)

| Lead | Iron | Chromium |
| --- | --- | --- |
| Nickel | Oxygen | Aluminium |
| Carbon |  |  |

Image 4

1. linescan

|  | Element Number; Element Symbol; Element Name; Atomic Conc.; Weight Conc.. 82; Pb; Lead; 16.77; 46.25. 26; Fe; Iron; 36.60; 27.21. 28; Ni; Nickel; 12.18; 9.51. 24; Cr; Chromium; 11.41; 7.90. 83; Bi; Bismuth; 1.30; 3.62. 8; O; Oxygen; 15.71; 3.34. 13; Al; Aluminium; 6.03; 2.17. |
| --- | --- |

FOV: 28 µm, Mode: 15kV - Map, Detector: BSD Full, Time: FEB 1 2023 08:30

Disabled elements: B, C, F, La, S

Cut out of line scan (resolution: 512 points)

| Iron | Lead | Oxygen |
| --- | --- | --- |
| Nickel | Chromium | Aluminium |
| Bismuth |  |  |

Combined line scan